**PART NUMBER JACKET REACTION REACTION AFTER**

A132412-DS-ND PVF 2.2 inches 4mm bounce

A132363-ND ETFE 2.4 inches full bounce

CN160GY-25-ND PPE 2.5 inches 10mm bounce

C2003V-5-ND PVC 2.1 inches full bounce

CN119R-25-ND SIL RUB 2.5 inches no bounce

T1327-1-ND TPU 2 inches 1mm bounce

CN481Y-25-ND XLPVC 2.8 inches 3mm bounce

CN112B-25-ND FEP 2.9 inches full bounce

**PART NUMBER FORM AFTER CREASE FORM AFTER SPIRAL JACKET FEEL**

A132412-DS-ND kept its form loose spiral ridged

A132363-ND kept its form very loose spiral ridged

CN160GY-25-ND loose form loose spiral soft

C2003V-5-ND tight form tight spiral very ridged

CN119R-25-ND loose form very loose spiral soft

T1327-1-ND no form no spiral very soft

CN481Y-25-ND tight form very loose spiral soft but ridged

CN112B-25-ND loos form loose spiral ridged